## Slide 1: Copper texture XRD Analysis SG-00005 6/7/23
EFK X-Ray Lab
T. Avbovbo,

## Slide 2: SG-00005
4 wafer samples were tested to check for preferred Cu (111) orientation.
  46KDN139SJB3 – Shortened to SJB3 in the report
  46KDN140SJE4 – Shortened to SJE4 in the report
  46KDN145SJD5 – Shortened to SJD5 in the report
  46KDN143SJC4 – Shortened to SJC4 in the report

## Slide 3: Wafer ID: SJE4
The Copper (111) planes have a preferred orientation with low intensity.
The (200) planes are randomly oriented with similar intensities as the (111) set of planes.
(111)
(111)
(200)
(200)

## Slide 4: Wafer ID : SJD5
The copper (111) planes have a preferred orientation with medium intensity.
The copper (200) planes have random orientation with low intensity.
(111)
(111)
(200)
(200)

## Slide 5: Wafer ID: SJB3
The copper (111) planes have a preferred orientation with high intensity.
The copper (200) planes have preferred orientation not parallel to the surface of the sample and low intensity.
(111)
(111)
(200)
(200)

## Slide 6: Wafer ID :SJC4
The copper (111) planes have a preferred orientation with high intensity.
The copper (200) planes have preferred orientation not parallel to the surface of the sample and low intensity.
(111)
(111)
(200)
(200)

## Slide 7: SJB3 V SJD5
The intensity of the (111) set of planes in SJB3 is 5 times greater than that of SJD5 (more (111) planes in SJB3 sample).
The intensity of the (200) set of planes in SJB3 is 5 times greater than that of SJD5 (more (200) planes in SJB3 sample).
SJB3
SJD5
SJB3
SJD5

## Slide 8: SJC4 V SJD5
The intensity of the (111) set of planes in SJC4 is 5 times greater than that of SJD5(more (111) planes in SJC4 sample).
The intensity of the (200) set of planes in SJC4 is 5 times greater than that of SJD5 (more (200) planes in SJC4 sample).
SJC4
SJD5
SJC4
SJD5

## Slide 9: SJB3 V SJE4
The intensity of the (111) set of planes in SJB3 is 3 times greater than that of SJE4 (more (111) planes in SJB3 sample).
The intensity of the (200) set of planes in SJB3 is 3 times greater than that of SJE4 (more (200) planes in SJB3 sample).
SJB3
SJE4
SJB3
SJE4

## Slide 10: SJC4 V SJE4
The intensity of the (111) set of planes in SJC4 is 3 times greater than that of SJE4 (more (111) planes in SJC4 sample).
The intensity of the (200) set of planes in SJC4 is 3 times greater than that of SJE4 (more (200) planes in SJC4 sample).
SJC4
SJE4
SJC4
SJE4

## Slide 11: Lotgering Factor
Wafer ID | LF
SJE4 | 0.81
SJD5 | 0.63
SJC4 | 0.93
SJB3 | 0.87
Lotgering Factor(LF) is a representation of orientation degree using XRD peaks.
LF =
P: Fraction of the summation of peak intensities corresponding to preferred orientation
: P with random distribution
LF =1 perfect preferred orientation
LF =0 random orientation
[1]
Wafer ID SJC4 has the highest degree of preferred orientation((111) plane)

## Slide 12: Future Work
Use Bruker XRD to calculate volume fraction of Cu (111) planes

## Slide 13: SJC4 V SJB3
The intensity of the (222) set of planes in SJB3 is 3 times greater than that of SJC4 (more 222 oriented planes in SJB3 sample).
SJB3
SJC4

## Slide 14
Tilt at 0 degrees
Tilt at 90 degrees
Tilt at 0 degrees
Tilt at 90 degrees
Tilt at 90 degrees
The (111) copper planes have a high intensity parallel to the surface of sample hence the bright red spot in the center
Alpha graph shows the 111 planes are mostly oriented to the surface of the sample